Specification sheet (example)

DEEP GROOVE BALL BEARING

Ref: SS ABC DGBB- d/m/y

| Relative documents | Supplier Manual | SM ABC d/m/y |
| --- | --- | --- |
|  | Inspection Program | IP ABC DGBB- d/m/y |
| Material | Outer Ring | 100 Cr 6 |
|  | Inner Ring |  |
|  | Rolling Elements |  |
| Hardness | Outer Ring | HRc 58-62 |
|  | Inner Ring |  |
|  | Rolling Elements | HRc 60-66 |
| Tolerance |  | P0 |
| Noise |  | Z1 |
| Vibration |  | V1 |
| Grease fill |  | 25-35% |
| Marking |  | ABC |

Residual Magnetism

| Bearing Outer diameter (mm) | ＞ |  | 30 | 50 | 120 | 250 |
| --- | --- | --- | --- | --- | --- | --- |
|  | ≤ | 30 | 50 | 120 | 250 | 430 |
| Max. Magnet Residue(mT) |  | 0.4 | 0.5 | 0.6 | 0.8 | 1.0 |